Total No. of Pages:  1

Register Number:                                                       					       7761

Name of the Candidate:

Diploma EXAMINATION - 2013

(welding engineering and technology)

(Paper-IV)

140. welding metallurgy and weldability testing

May)                                           Maximum: 100 Marks	        	      (Time: 3 Hours

Answer any five questions		             (5×20=100)

|  | a) Derive an expression for heat flow in welding. b) Discuss TTT and CCT. |
| --- | --- |
|  | a) Explain in detail about the significance of carbon equivalent steels. b) Briefly discuss the problems encountered while welding HSLA steels. |
|  | a) Explain in detail about the difficulties found during welding of aluminium and its alloys. b) Describe in detail about various weldability process for non-ferrous materials. |
|  | a) Write the factors which may promote stress corrosion cracking? Explain hot crack. b) Explain in detail about the controlling of distortion in weldments. |
|  | a) Explain controlled thermal severity test. b) Describe in detail about controlled severity test. |
|  | a) Write short notes on bent test and nick break test. b) Briefly discuss about the problems occurred while conducting cold crack test. |
|  | a) Briefly discuss about aging and tempering. b) Write about various welding zone. Explain any two. |
|  | a) Explain in detail about varestraint test. b) Write short notes on NDT? Explain acoustic emission testing. |

~~~~~~~~~~~